## Slide 1: Quantum Dot Intersubband Photodetectors for LWIR photons
Stefano Vichi, S. Asahi*, S. Bietti, A. Tuktamyshev, A. Fedorov**, T. Kita* and S. Sanguinetti
Materials Science Department, University of Milano-Bicocca, Milano (Italy)
* Department of Electrical and Electronic Engineering, Kobe University, Kobe (Japan)
** L-NESS & CNR-IFN, Milano (Italy)

## Slide 2
Rogalski et al., J. Appl. Phys. 105, 091101 (2009)
High uniformity on big areas
Lower production costs
Higher density of pixels
Uncooled (or Peltier) detection
Mature technology
High quantum efficiency (~70%)
Can be tuned in the range 1-30 µm
Low growth uniformity
Extremely high cost
HgCdTe

## Slide 3
Rogalski et al., J. Appl. Phys. 105, 091101 (2009)
QWIP (Quantum Well)
High uniformity on big areas
Lower production costs
Higher density of pixels
Uncooled (or Peltier) detection
Multispectral imaging
Mature technology
Short carrier lifetime (lower quantum efficiency)
Only IR radiation parallel to the QW is detected
High growth uniformity
Lower cost

## Slide 4
Rogalski et al., J. Appl. Phys. 105, 091101 (2009)
QDIP (Quantum Dot)
Technology based on well estabilshed GaAs technology
High optical absorption at normal incidence
Low dark current due to lower thermal emission
Possible high operating temperature (Peltier cooling -80°C)

## Slide 5
The decrease in detectivity with temperature is a crucial issue.
Up to now external cooling is always required to improve S/N ratio.
Increased complexity
Reduced device lifetime in space satellites

## Slide 6
QDIP are promising but not yet competitive.
Large dark current at room temperatures
Low density of absorbers
Barrier
Intraband transitions

## Slide 7
Small capture
Low thermalization efficiency (phonon bottleneck)
Low escape probability (phonon bottleneck)
Large absorption coefficient
Ok extraction (tunneling)
Increase capture and thermalization efficiencies without increasing the escape probability.
Capture and thermalization are very efficient in 2D nanostructures.
0D nanostructures have low escape probability and high absorption coefficient.
What if we can combine these advantages?

## Slide 8
We designed and realized by Droplet Epitaxy a hybrid 0D-2D nanostructure (QDs on top of a QW) made of GaAs/AlGaAs.
The absence of a potential barrier between 0D and 2D allows to spatially modulate the properties quantum confinement.
QD-like low energy states
QW-like high energy states
2D
2D
0D

## Slide 9
Vichi et al., ACSPhotonics 12,447−456 (2025)
The QW introduces resonant states in CB, E>ECB with a localization in the QD region -> large absorption probaility

## Slide 10
Small capture
Low thermalization efficiency (phonon bottleneck)
Low escape probability (phonon bottleneck)
Large absorption coefficient
Ok extraction (tunneling)
Large capture
High thermalization efficiency (carrier-carrier scattering)
Low escape probability (phonon bottleneck)
Good absorption coefficient
Large extraction (resonant states)
Vichi et al., ACSPhotonics 12,447−456 (2025)
≠ℏωLO

## Slide 11
Two-step growth of self-assembled QDs:
Deposition of group III to form metal droplets
Crystallization with group V flux
Advantages:
Strain-free growth
Independent control on QD morphological parameters (height, aspect ratio, shape)
Narrow size dispersion
Gurioli et al., Nat. Mater. 18, 799 (2019)
AlGaAs
AlGaAs
GaAs
20 nm
Keizer APL 96 (2010) 62101
Droplet Epitaxy
Notes: DE uses growth kinetics to form QD.

## Slide 12
RT dark current
QD density = 7*1010 cm-2
Room temperature absorption signal detectivity = 2*10-4 A/W at -4 V

## Slide 13
CONCLUSIONS:
Innovative quantum state design to modulate quantum confinement:
- 0D ground state
- 2D excited states
To exploit the advantages of both nanostructures.
Achieved room temperature operation R = 2*10-4 A/W
Vichi et al., ACS Photonics 12,447−456 (2025)

## Slide 14
EXTRA SLIDES

## Slide 15
15
Droplets
Ga, In, Al… molecular beam
Flux
Temperature
0.1 ML/s
300 °C
Ga flux constant, increasing T
T constant, increasing Ga flux
Ga droplet deposition
Notes: 15
15

## Slide 16
Droplet deposition:
Ga amount --> droplet volume
Temperature --> droplet density
Crystalization controls geometry:
As incorporation in the droplet and crystalization at the liquid-solid interface
As adsorption on the surface and crystalization after Ga out-diffusion
Diff. length
Diffusivity
Lifetime
DE-QDs formation
Notes: DE uses growth kinetics to form QD.
In step 1 there is an initial formation of the ring

## Slide 17
How to change R without changing h?
Increase diffusion length
How to change h without changing R?
Increase droplet volume
5x10-5 torr
1x10-5 torr
5x10-6 torr
150 °C
200 °C
250 °C
DE-QD shape engineering
Bietti et al., Phys Rev B 92, 075425 (2015)

## Slide 18: Aspect Ratio effect on LO phonon detuning
ħωLO=36 meV
ρ=0.26
ρ=0.12
QD: h≈3, 6 nm, D≈25
Aspect ratio
Steinhoff et al., Physical Review B 88, 205309 (2013)
ΔE=40 meV
ΔE=20 meV
QD-IBSC: engineering of carrier dynamics
Scaccabarozzi et al., Prog Photovolt Res Appl. 31, 637 (2023)