## Slide 1: Missione 4 Istruzione e Ricerca
Development and Analysis of Transmon Qubits: Design, Simulation, and Characterization
Danilo Labranca
danilo.labranca@mib.infn.it

## Slide 2: Interest in light Dark Matter
DM particles with
Candidates
  Axion: Peccei-Quinn symmetry breaking  would solve the strong CP symmetry problem
  Dark photon: from extensions of Standard Model  a massive particle that mixes with the photon
Both candidates can convert into photons at frequencies that depend on the DM particle mass
Transmon qubits are sensitive to weak EM fields at GHz frequencies

## Slide 3: Transmon as single photon detector
Detection through Ramsey sequence
QND detection  reduction in dark counts
Single Photon
No Photon
Nature Phys 14, 546–549 (2018)
Phys. Rev. Lett. 126, 141302 (2021)

## Slide 4: Transmon qubit chip design
Need good prediction of the detector parameters
First design focuses on simulation-experiment agreement
Two non-interacting qubits
One is tunable with external flux and can be driven directly with a dedicated drive-line
Each qubit features a simple coplanar resonator for readout
A. Sirois, M. Castellanos, D. Olaya, J. Bieseker, P. Hopkins, S. Benz.

## Slide 5: Transmon qubit chip design
Need good prediction of the detector parameters
First design focuses on simulation-experiment agreement
Two non-interacting qubits
One is tunable with external flux and can be driven directly with a dedicated drive-line
Each qubit features a simple coplanar resonator for readout
Readout resonator
Qubit
A. Sirois, M. Castellanos, D. Olaya, J. Bieseker, P. Hopkins, S. Benz.

## Slide 6: Transmon qubit chip design
We need good prediction of the detector parameters
First design focuses on simulation-experiment agreement
Two non-interacting qubits
One is tunable with external flux and can be driven directly with a dedicated drive-line
Each qubit features a simple coplanar resonator for readout
Readout resonator
Qubit
Josephson Junction
Coupler
Capacitance
A. Sirois, M. Castellanos, D. Olaya, J. Bieseker, P. Hopkins, S. Benz.

## Slide 7: Chip simulation
Lumped Oscillator Model (LOM)
  Ansys Q3D extract the capacitance matrix of the qubit and the coupler
Energy Participation Ratio (EPR)
  Ansys HFSS to extract the resonant frequencies of the circuit
Both methods lead to the main Hamiltonian parameters of the circuit

## Slide 8: Chip simulation
Lumped Oscillator Model (LOM)
  Ansys Q3D extract the capacitance matrix of the qubit and the coupler
Energy Participation Ratio (EPR)
  Ansys HFSS to extract the resonant frequencies of the circuit
Both methods lead to the main Hamiltonian parameters of the circuit

## Slide 9: Chip simulation
Lumped Oscillator Model (LOM)
  Ansys Q3D extract the capacitance matrix of the qubit and the coupler
Energy Participation Ratio (EPR)
  Ansys HFSS to extract the resonant frequencies of the circuit
Both methods lead to the main Hamiltonian parameters of the circuit

## Slide 10: Measurement setup

## Slide 11: Resonator spectroscopy
At high power:
  The qubit energy levels are saturated
  The resonator behaves like it is alone in the chip
At low power:
  The qubit is in the ground state and interacts with the resonator
  The distance between the bare and dressed frequencies is
 | GHz
HFSS | 

## Slide 12: Qubit spectroscopy
One tone (readout tone) at GHz is used to continuously readout the resonator (the )
A second microwave tone (drive tone) is used to scan for the qubit frequency
The changes when the qubit gets excited by this second pulse
= MHz

## Slide 13: Control pulse calibration
The calibrated pulses are:
  -pulse: prepares the qubit
  -pulse: prepares the qubit
-pulse
ns

## Slide 14: Frequency tunable transmon
Resonator and qubit spectroscopy as a function of flux bias
Resonator spectroscopy shows the avoided crossing
The full characterization is performed at the minimum frequency
Resonator spectroscopy
Qubit spectroscopy
from fit

## Slide 15: Relaxation time measurement
The relaxation time is the mean time necessary for the qubit in the to spontaneously relax into the state

## Slide 16: Coherence time measurement
The decoherence time is the mean time necessary for the qubit to lose the phase information
With MHz
ns

## Slide 17: Spin-Echo measurement
Focusing 𝝅-pulse at half pulse sequence refocuses the state
Removes the inhomogeneous dephasing

## Slide 18: Relaxation and Coherence time measurement
These measurement were performed multiple times (about 24 hours) for both qubits
The Purcell limit on the is approximately
The limiting factor:
  Unoptimal setup
  Ground loops
  Substrate and interface losses
 | Fixed frequency qubit | Tunable qubit
 | ns | ns
 | ns | ns
 | ns | ns
 | Fixed frequency qubit | Tunable qubit

## Slide 19: Summary of qubit characterization
Parameter | LOM | EPR | Experiment
 | nH (Fixed) | nH (Fixed) | nH (Estimate)
 | GHz | GHz | GHz
 | MHz | MHz | MHz
 | GHz | GHz | GHz
 | kHz | kHz | kHz
 | MHz | MHz | MHz
Parameter | LOM | EPR | Experiment
Fixed frequency
qubit
Tunable frequency
qubit
Parameter | Estimate | Fit
Parameter | Estimate | Fit

## Slide 20: Summary of results and next steps
The simulation-experiment agreement is very good:
  Within 6% for frequencies and 2% for dispersive shifts
The performance are not as high as expected
  and are limited to about and respectively
  The Purcell limited is and does not justify the measured values
Possible causes for the lower performance:
  Unoptimized setup (no IR filters, low attenuation, ground loop)
  Additional unaccounted losses (interfaces and substrate)
Measure the exact same chip again adjusting the measurement setup
The measurement on the right were performed on the same design but in a different setup

## Slide 21
Thank you!
D. Labranca, R. Moretti, P. Campana, R. Carobene, M. Gobbo, M. A. Castellanos-Beltran, D. Olaya, P. Hopkins, L. Banchi, M. Borghesi, A. Candido, S. Carrazza, A. Cattaneo, H. A. Corti, A. D’Elia, M. Faverzani, E. Ferri, S. Gamba, A. Nucciotti, L. Origo, A. Pasquale, A. S. Piedjou Komnang, A. Rettaroli, S. Tocci, C. Gatti, A. Giachero

## Slide 22: Backup slides

## Slide 23: Light DM conversion into photons
Axions:
Inverse Primakoff effect
  In resonant cavities with
  Large fields  conversion probability scales as
Dark photons:
Kinetic mixing
  In resonant cavities with
  No need for fields
https://doi.org/10.1103/PhysRevD.110.043022
https://doi.org/10.48550/arXiv.2403.02321

## Slide 24: Dark Matter evidences
Galaxy rotation curves
  Visible matter does not explain the rotational speed of galaxies at large distances from the center
Cosmic Microwave Background (CMB)
  Measurements of the CMB anisotropies support the ΛCDM model with dark matter
Galaxy clusters
  Velocity of galaxies within cluster is too high to be explained by visible matter (as well as velocity dispersion)
Gravitational Lensing

## Slide 25: Qubit Spectroscopy

## Slide 26: dc-Squid inductance

## Slide 27: Rabi oscillations

## Slide 28: Dispersive shift

## Slide 29: Relaxation and Coherence time measurement

## Slide 30: Relaxation and Coherence time measurement
 | Fixed frequency qubit | Tunable qubit
 | ns | ns
 | ns | ns
 | ns | ns
 | Fixed frequency qubit | Tunable qubit

## Slide 31: Light DM conversion into photons
Axions: itinerant photon detection scheme
Dark photons: localized dection scheme
Resonator + Qubit
Axion conversion cavity
Transmission line
Dark photon conversion cavity
Readout cavity