## Slide 1
PNRR Partenariato Esteso
NATIONAL QUANTUM SCIENCE AND TECHNOLOGY INSTITUTE “NQSTI”
Spoke 6 Quantum Integration
A6.3.3 Superconducting quantum networks
A6.3.3.1 Mikhail Lisitskiy SPIN CNR
A6.3.3.2 Berardo Ruggiero ISASI CNR
Low power microwave photon detector based on Superconducting Qubit Network
Mikhail Lisitskiy
SPIN- CNR Institute of Superconductors, Innovative Materials and Devices,
mikhail.lisitskiy@spin.cnr.it
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025

## Slide 2
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Valentina Di Meo1, Berardo Ruggiero2, Carmela Bonavolontà2, Paolo Vanacore2, Claudio Gatti3, Fabio Chiarello4, Giorgio Brida5, Emanuele Enrico5, Luca Fasolo5, Luca Oberto5, Mikhail Fistul6, Gregor Oelsner7, Eugeni Ill’chev7, Patrick Navez8, Alexandre Zagoskin8, and Paolo Silvestrini9,2
1. SPIN CNR ,Via Campi Flegrei 34, I- 80078, Pozzuoli (Naples), Italy
2. ISASI CNR ,Via Campi Flegrei 34, I- 80078, Pozzuoli (Naples), Italy
3. LNF INFN , Via Enrico Fermi 54, I- 00044 , Frascati (Rome), Italy
4. IFN CNR , Via Fosso del Cavaliere 100, I- 00133 , Rome, Italy
5. INRiM, Strada delle Cacce 91, I-10135 , Turin Italy
6. Ruhr University Bochum, Universitätsstraße 150, D-44801, Germany
7. Leibniz Institute of Photonic Technology, Albert-Einstein-Straße 9, D-07745 Jena, Germany
8. Loughborough University, LE11 3TU, Loughborough, United Kingdom
9. Università degli Studi della Campania “L. Vanvitelli”, Dipartimento di Matematica e Fisica, Viale Lincoln 5, I- 81100 Caserta, Italy
Co-authors of the presentation:

## Slide 3
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
State of the art of conventional microwave detectors
Low-barrier Schottky diode (LBSD)
Agilent LBSD 8484A
Power range:
-70 dBm (100 pW) to -20 dBm (10 mW)
Frequency range:
10 MGz -18 GHz

## Slide 4
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Theory of SQN detector based on collective quantum states
Theoretical setup of the SQN detector.
M.V.Fistul et al, Phys. Rev. B, 105, 104516 (2022))
ac Stark effect (in electric field)
is average qubit frequency
γ is the coupling strength between a single qubit and a resonator
A generic quantum-mechanical model of disodered interacting SQN coupled to a low-dissipative resonator and transmission line
An amplitude of the main resonance drastically increases as the interaction overcomes the disoder, and the collective state is formed
In the presence of a weak non-resonant photon electric field, the position of resonances depends on the number of photons, i.e. the collective ac Stark effect is obtained
blue line n=0
red line n=1
green line n=2

## Slide 5
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Single microwave photon
with frequency ωph
|0>
|CS>
E
Magnetic field
ΔωSℏ
ωcℏ
ωqℏ
ΔωS
- Stark shift related to a single MW photon
Coherent collective
quantum state
S21
ωc-ΔωS
ω
ωc
ωph
Working principle of the SQN detector of a single microwave photon
A SQN embedded in a resonator produces collective quantum states.
In the presence of external microwave signal the frequency shift of the collective mode takes place because of the AC Stark effect.

## Slide 6
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
T-type two resonator SQN with 10 capacitor shunted flux qubits
The resonators are fabricated by depositing a 200 nm thick Nb film on a silicon substrate that is structured by the RIE. The flux qubits are made of Al Josephson-junctions fabricated by two angle shadow evaporation technique. Every flux qubit of the SQN consists of a 6x4.5 μm2 loop with three Josephson junctions. Two junctions are designed to have identical size of 0.2x0.87 µm² while the third is scaled by a factor α < 1. For qubits of the SQN measured here, the factor α = 0.8.
The Leibniz Institute of Photonic Technology (Leibniz IPHT), Jena Germany
SEM picture of the coplanar capacitor which connects the S-resonator with T-resonator. 10 qubis are embidded inside the coplanar capacitor
Zoomed SEM image of the flux qubit loop
Optical image of the T-type SQN with 10 C-shunted flux qubitswith two resonators
SEM image of five flux qubits shunted by coplanar capacitors

## Slide 7
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Microwave part of experimental set-up
Experimental set-up for double tone microwave measurements of the T-type SQN
Cabling of T-type three terminal device
Measurements of fabricated T-type SQN were carried out at the National Laboratory of Frascati (LNF) (Italy) in a Leiden Cryogenics CF-CS110-1000 dilution refrigerator at temperature of 15 mK.
SQN
Port 3
Port 1
Port 2
Readout resonator
Signal
resonator

## Slide 8
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Dependence of the frequency position of the resonant drop reported in left figure as a function of the power of the second-tone signal.
First-tone Port 1-Port 2 -transmission coefficient S21 vs VNA-frequency dependencies recorded at different powers of the second-tone signal of frequency of 7.74328 GHz applied to the Port 3 (increasing of power). T=15 mK , zero magnetic field.
Port 1
Port 2
Port 3
Measurement of two-tone spectra of the T-type two resonator SQN -device
First tone signal for measurements of transmission coefficient S21 between port 1 and port 2 of the readout resonator : VNA outputpower was -40 dbm, (-100 dbm at the device)
Second tone signal of different power and frequencies: Rohde & Schwarz SMA100B was connected to the Port 3 of the signal resonator. The output power of the generator was varied from -40 dbm to -20 dbm. Frequency variation was from 7.741 GHz to 7.751 GHz

## Slide 9
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Experiment on dip position of the first tone S21 frequency dependence on power and frequency of the second tone signal.
We observed the sensibility of the frequency position of the resonant drop both to the power of pump signal and to pump signal frequency.

## Slide 10
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Evolution of the first tone S21 with increasing second tone power for bistability
dependences.

## Slide 11
Theoretically predicted values of frequency shift versus the input power in dBm
Theoretical model is based on a non-linear multiphoton interaction between pump microwave signal and a qubit system of the SQN where the frequency shift is the sum of the multiphoton AC Stark shift values of each qubit. (P. Navez et al, in preparation).
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Theoretical description of the dip position on the signal power

## Slide 12
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Photon number calculation
N is the average number of photons per period stored in the sensing resonator
P3 is the second tone power applied to the sensing resonator
Ql is the loaded quality factor
Qc is the coupling quality factor
f0 is a resonant frequency
𝑄𝑐=|𝑄𝑐|exp(−𝑖𝜙)
Defrance F. et al, Physical Review Materials,
8(3) (2024)
Chen Q. et al ,
Phys. Rev. B, 106 (21)
(2021)

## Slide 13
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Average number of photons per period stored in the sensing resonator

## Slide 14
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
N-110 ≈ 72,91 f-110 = 7.746295 GHz
N-109 ≈ 91,79 f-109 = 7.746285 GHz
σ = = 0.53 kHz/photon
N-101 ≈ 579 f-101 = 7.74595 GHz
N-100 ≈ 729 f-100 = 7.74588 GHz
σ = = 0.46 kHz/photon
Sensitivity without bistability

## Slide 15
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Sensitivity with bistability
N-90 ≈ 7.29*10^3 f-90 = 7.745265 GHz
N-89 ≈ 9.18*10^3 f-89 = 7.74335 GHz
σ = = 1 kHz/photon
N-101 ≈ 579 f-101 = 7.745735 GHz
N-100 ≈ 729 f-100 = 7.744985 GHz
σ = = 6 kHz/photon

## Slide 16
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
Microwave power range: SQN detector –vs- Schottky diode detector
-110 dBm - -75 dBm @7.748 GHz
-30 dBm - -15 dBm @5.5 GHz
Agilent LBSD 8484A
-70 dBm - -20 dBm @10 MGz -18 GHz

## Slide 17
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025
We theoretically predicted and experimentally demonstrated that SQN detector with collective quantum state permits to detect a low power microwave signal with a frequncy of 7.748 GHz in the range between -110 dBm and -75 dBm which is lower than the microwave power range of conventional Schottky detector.
The detector sensitivity of SND device is suitable to count a few photons with a frequencies related to bistability regime.
Conclusions

## Slide 18
Thank you for your attention!
Secondo Congresso Nazionale di NQSTI Roma , 07 Febbraio 2025